### ALFAPOL АМШ

DRY FLOOR SEALING BEARING RADIO SCREENING ANTIELECTROSTSTIC FIRE-PROOF MORTAR MAGNESIAN MIXTURE М200  ПК3

For creation of radio screening antielectroststic floor covering.

Patent for invention #32 233 255. Sanitary-epidemiological conclusion # 78. 01.06.574.П.016079.09.09  TU № 5745-001-82166262-2001

Not liable to obligatory certification. Does not included into “List of the products liable to obligatory certification in relation to fire safety”

In accordance with the requirements of GOST 12. 4.124-83 for antielectrostatic materials.

Destination

This mixture is used for screening of electromagnetic fields in radio frequency range, protection from static electricity, electric fields of industrial frequency, solving of the problems connected with electromagnetic compatibility of technical means, protection of means and systems of information processing, excluding of information leaks through technical channels.

Objects of application

( plants of electronic industry;

( plants of radio engineering and instrument making industry;

( plants of medical industry;

( computer centers, server rooms;

( rooms for individual use (residential rooms and offices);

( medical institutions and sanatoriums;

( rooms where the protection from static electricity should be ensured;

( rooms to be under influence of electromagnetic fields;

( sport centers;

( rooms to be under expressed influence of anomalies of natural fields (geodynamic active areas of geological breaks;

( rooms for army duty officers and other force structures, dispatcher of power plants, airports etc;

( treatment-preventive institutions.

Advantages

( screens electric fields 50 Hz and electromagnetic radiations in wide frequency range (from 10 kHz up to several dozens GHz), depending upon thickness of layer the effectiveness of screening of material is up to dozens dB.

( has features of absorbing of electromagnetic radiations;

( does not accumulate static electricity;

( does not distort magnetic field of Earth. It ensures natural geomagnetic conditions in buildings and at working places. The rooms equipped with magnesian-shungite coverings have relaxation and health-improving effect. These rooms are used for restorative therapy;

( ensures smoothing of concrete and cement-sand underlays;

( relates to category of not dusting and noncombustible materials;

( has increased adhesion to underlays as well as elasticity and а crack growth resistance;

( has dimensional stability and high strength to be inherent for all magnesian compositions ALFAPOLтм;

( is frost resistant, may be used in not heated rooms;

( is repairable

( has ecological composition.

General requirements

Observe the requirements of SNiP 2.03.13-88 “Floors” and SNiP 3.04.01-87 “Insulating and finishing coatings” during execution of works. In case of the use of “ALFAPOL АМШ” for protection from electromagnetic fields the requirements of the following norms:

1 – SanPiN 2.2.4.1191-03 “Electromagnetic fields in industrial conditions”,

2- SanPiN 2.1.8/2.2.4.1190 – 03 “Hygienic requirements for placement and operation of means of land and moving radio communication”

3- SanPiN 2.1.8/2.2.4.1383 – 03 “Hygienic requirements for placement and operation of transmitting objects of radio equipment” should be observed.

At that the requirements of GOST Р 51318.14.1-99 and GOST Р 51318.14.2-99 related to electromagnetic compatibility of household appliances, electric tools and analogous devices household appliances should be taken into account.

During the whole period of implementation of work the temperature of the room should be no less than +10°С, relative humidity in the room should not exceed 60%. The change of temperature and relative humidity in the room will change the period of “dry-setting”. The mixture is to be laid onto dry “mature“ (1-3 months) concrete underlay or onto 28-days cement-sand covering. It is not permitted to apply the mixture onto newly placed cement covering.

Рreparation of a surface of the basis

Note

In order to ensure the screening coefficient at level no less than 60 dB the brass (steel) lath with mesh 2x2 mm should be laid on the floor. The overlay of lath should be equal to 100 mm. The joint should be soldered or glued with the use of conductive adhesive, and pressed to the wall with the use of self-threading screws through copper bar. The copper bar should be connected to grounding circuit. The thickness of the layer of “ALFAPOL АМШ” should be equal to 15-20 mm in this case. The grounding circuit should be implemented in accordance with “Rules for protection from static electricity”.

Mount the pads made of damping materials (thickness no less than 5 mm) in the places of joining to walls and columns as well as places of passage of communications. Remove abrasive unstable, loose and loosened areas of underlay. The surface should be cleaned from “cement milk”, dust, oil, paint and other substances preventing gluing of smoothing mixture. If necessary the underlay should be milled. Three-four hours before laying of mixture the cracks and large dents (preliminary pointed and primered ones) located at the floor underlay should be sealed with the use of material “ALFAPOL МБ” or with the use of the same mortar. The displaced metal parts should be processed with bituminous varnish. Mount the guides. These guides should be fastened to the floor with the use of self-threading screws or with the use of mortar "ALFAPOL АМШ". The prepared surface should be thoroughly grounded with the use of primer "ALFAGRUNT - АЛЬФАГРУНТ" or analogous one 2-3 times. Each layer of primer should be impregnated into underlay and dried during 4-6 hours at room temperature (see Instruction for primer). Do not use polyvinylacetate or other alkali containing primers.

Рreparation for use

Before implementation of the work the temperature of tempering agent and dry mixture should be no less than +10 °С. The clean plastic (metal) reservoirs 30-100 l should be used for mixing with the use of mixer.

The mortar mixture consists of two factory made components and water:

1. Bag of dry mixture "ALFAPOL АМШ" - 25 kg.

2. Tempering agent (bischofite)

3. Water

The bischofite should be poured into reservoir (mortar mill), ___ liters of water (at room temperature) should be added, then one bag of dry mixture should be charged into reservoir. All these components are to be mixed during 2-3 minutes. The quantity of water and bischofite are indicated in the stamp on the bag. Settle the produced mixture 2-3 minutes, then perform the repeated mixing – in order to achieve complete homogeneity. Pour this composition out of the reservoir onto the prepared surface.

Еxpense of a dry mix

The consumption of dry mixture equals to 16 kg for 1 m2 (for thickness of layer 10 mm).

Рrotection

During implementation of work the usual security measures for protection from dust (respirator) should be observed. The solution of bischofite is to be washed from open places with water. The solution of bischofite is to be washed from open places with water.

ATTENTION!

- Use of concrete mixers for batching is not permitted.

- Speed of rotation of mixer should be in range from 400 up to 600 rpm.

- In order to prevent cementation it is not permitted to store the mixture in the reservoir for a long time.

Quality control

In order to determine the quantity of the liquid in the mixture as well as ensure better compliance with existing underlay, primer, temperature, humidity and other conditions we recommend to perform trial laying of mortar (1 bag).

Рerformance of work

The mortar mass “ALFAPOL АМШ” is to be laid onto preliminary mounted guides of required height (as stripes). In case of the presence of large gaps between guides and floor the gaps should be preliminary sealed outwards of stripe with the use of the ready-to-use mass - in order to prevent leakage of mortar. The width of the stripe is to be chosen according to actual conditions. In case of laying onto large areas the implementation of isolation joints in concrete should be repeated. The optimal thickness of layer - 15-30 mm.

The mortar mass is to be taken out of the mixer, laid onto coated stripe and stretched with the use of straightedge striker on the guides. At that the surface should be smooth one and free from any grooves and cavities. The period of the work with mortar (till the beginning of cementation) equals to nearly 40 minutes at room temperature. The guides should be taken out of the mortar before final hardening of this mortar. The created cavities are to be filled up with the use of the mortar mixture.

After achieving of “readiness” of material (small pits are created due to pressing by hand with moderate force) the smoothing of the material should be performed (manually or with the use of concrete-finishing machine without usage of liquids). The beads of fresh mortar located at previously laid stripe should be scraped during implementation of smoothing at the places of the joints.

Рrotection

The tools should be washed with water after implementation of work.

The hardening of the composition should be performed in dry environment. The room is to be ventilated. During process of hardening the moistening of covering (polishing with water) is not allowed.

The heterogeneity of color of a covering (from light- gray up to dark- gray) is possible, particularly in the places of joints of stripes. It does not exert influence on properties of a covering.

Packaging, storing and operation

The dry mixture "ALFAPOL АМШ" is delivered as complete units in paper bags 25 kg each. The tempering agent (bischofite) is delivered in barrels or canisters.

The warranty period of storage -6 monthsfrom the date of production. The mixture should be stored in dry room without allowing hit of direct sunshine.

During operation of floors the following should be taken into account:

- humid cleanup of floor is only allowed no sooner than 7 days after laying.

- cleanup of rooms with application of water hoses is not performed;

- washing of floors is to be performed with the use of washing liquid.

The repair of the floor during operation should be performed according to this Instruction.

The manufacturer has no responsibility for improper use of material as well as for use of the material not to be in accordance with its destination.

## TECHNICAL DATA

| Thickness of one layer for one pass | from 15 up to 40 mm | Frost resistance, mark | F200 |
| --- | --- | --- | --- |
| Material consumption for layer 10 mm | 16 kg. for 1m2 | Wearability of smoothed mortar, no more than | 0.7 g/cm2 |
| Time of suitability of mortar to use | 40 min | Category of combustibility, GOST 30244-94 | НГ |
| Temperature of application | from +10˚С up to +25˚С | Radiation standards (НРБ-99) | 1 class |
| Compression strength, no less than | 20 MPa | Specific volume electric resistance, GOST 12. 4..124-8, no more than | 10-7Ohm*m |
| Bending strength, no less than | 9 MPa | Specific surface volume electric resistance, GOST12. 4..124-8, no more than | 10-9Ohm*m |
| Strength of adhesion with concrete, no less than | 1 MPa |  |  |
| Fractions, maximum | 3 mm |  |  |
| Thermal conductivity | 0.96 W/m˚С | Coefficients of screening are indicated in registration certificate |  |